Flange Size: DN 40 CF (2.75" OD)
Alignment: Rotatable
Material: 304 Stainless Steel
Bore: 1.625"
Thickness: 0.500"
Bolt Circle: 2.312"
Bolt Hole Diameter: 0.266"
# Bolt Holes: 6
Vacuum Range: FKM: 1 X 10-8 mbar to 1 bar
Metal seal: 1 X 10-13 mbar to 1 bar
Temperature Range: FKM: -20 °C to 180 °C
Metal seal: -200 °C to 450 °C
Weight: 0.440 lbs