Flange Size: DN 100 CF (6" OD)
Type: Double sided
Alignment: Non-rotatable
Material: 304 Stainless Steel
Bore: Blank
Thickness: 0.780"
Bolt Circle: 5.128"
Bolt Hole Diameter: 0.332"
# Bolt Holes: 16
Vacuum Range: FKM: 1 X 10-8 mbar to 1 bar
Metal seal: 1 X 10-13 mbar to 1 bar
Temperature Range: FKM: -20 °C to 180 °C
Metal seal: -200 °C to 450 °C
Weight: 5.46 lbs