Viewport Type: Welded Zero Length Viewport
Flange Size / Type: DN 100 CF (6" OD)
Viewport Material: 7056 Glass
Flange Material: Stainless Steel
Vacuum Range: 1 X 10-10 mbar to 1 bar (UHV)
Temperature Range: -20 °C to 200 °C
Weight: 2.820 lbs